(

Mechanical properties of Cu/banana peel powder/HDPE as hybrid composite material

Aradhyula Thirumala Vasu1, Ram Narayan Chauhan1, 2, M. Ramakrishna1, Murthy Chavali3*.

Abstract— Hybrid nanocomposites have been prepared using the waste banana peels, copper nanoparticles as reinforcements and high-density polyethylene (HDPE) as a matrix by hand layout and casting methods.  Washed banana fibers and different wt. % of copper nanoparticles were properly mixed in HDPE via thorough stirring. After that, the resultant solution has been cast and dried to result in the hybrid nanocomposites. Their mechanical properties have been studied in details and compared with the conventional composite made from the waste banana peel used as reinforcement and high-density polyethylene (HDPE) as a matrix. The material can be used in the applications of Aerospace and Automobile etc.

Keywords— Banana peel powder, copper nanoparticles, and polyethylene matrix composite, and mechanical properties

- INTRODUCTION

Banana is one of the high calories, tropical fruits [Duan X, Cheng G, Yang E, et al. Modification of pectin polysaccharides during ripening of postharvest banana fruit. Food Chemistry, Volume 111, Issue 1, 1 November 2008, Pages 144-149; Nieman DC, Gillitt ND, Henson DA, et al. Bananas as an energy source during exercise: a metabolomics approach. PLoS One 2012; 7:e37479; www.nutrition-and-you.com/banana-fruit.html; www.whfoods.com/genpage.php?tname=foodspice&dbid=7; www.livescience.com/45005-banana-nutrition-facts.html] (Musa acuminata colla; Musaceae), contains lots of proteins and vitamins (mainly B6 and C) in it, after consuming the peel is left out as a waste. These banana peels contain natural fibers and which are eco-friendly. These have a property which supports in composites for improving its mechanical properties. India is one of the top three producers of banana, mainly from the states of Andhra Pradesh, Gujarat, Karnataka, Kerala, Maharashtra and Tamilnadu.

The composition of material includes high-density polyethylene (HDPE), copper and banana peel fiber. HDPE is from the family of polyethylene with a change in its physical states such as in molecular weight, molecular weight distribution, and density. By which physical properties of HDPE changes in flowability, rigidity, surface hardness, transparency, and melt tension. As compared with the low-density polyethylene, high-density polyethylene (HDPE) only chosen.

In the present work the banana fiber with high-density polyethylene and copper incorporation in the composite. The composite was analyzed by evaluating through undergoing tests on its mechanical properties. There are many applications after the properties were known, in the fields of aerospace and automobile, etc.  It serves with low cost and high performance comparatively.

- MATERIALS AND TECHNIQUES

Materials required for this composite are banana peel powder, copper nanoparticles, and high-density polyethylene. The cleaned banana peels dried in open air, the dried banana peels are made into powder. High-density polyethylene, the only type of polyethylene produced was low-density polyethylene. Low-Density polyethylene was produced at extremely high pressures. This high-pressure polymerization created polyethylene with many branches; these branches are created due to intermolecular and intermolecular chain transfer during polymerization. The mechanism involved for the polymerization of low-density polyethylene is free radical polymerization. The uses of low-density polyethylene are limited due to a high number of branches. Because of the extreme pressure needed to create low-density polyethylene and its limited uses, Karl Ziegler [Karal Ziegler Nature Materials 12, 773 (2013)] tried in creating polyethylene at atmospheric pressure. Were copper nanoparticles are prepared from copper strips using a ball milling machine.

Banana peel powder, copper microparticles and HDPE was used in ratios of, 5%-1%-94%, 10%-1%-8%, and 15-1%-84% respectively. The various methods used in testing of composite materials are a tensile test, bending test and impact test. The pieces were prepared in different concentrations and in different shapes by the process of injection molding and casting technique for testing. These prepared pieces were subjected to various mechanical tests like a tensile test, bending test and impact test.

- EXPERIMENTAL SYSTEM

The banana peel powder was collected from dried banana peels by grinding them. The collected powder was sieved from different mesh sizes. The banana shell powder and copper particles are incorporated with high-density polyethylene with the help of injection molding and casting technique with respective percentages of banana peel powder and copper particles. The ambient temperature of the high-density polyethylene is 200°C.The mixture was prepared into the required shape and size with the help of moulds of injection molding. All the specimens are to be undergone through above mentioned tests, hence, a total of 15 pieces are required, The dimensions and shapes of those pieces are in table1 The pieces are tested for the mechanical properties, the piece which is compared with the standard, the one which matches with the standard it is acceptable for application in various mechanical fields.

- RESULTS AND DISCUSSION

The experimental curves for tensile strength from tensometer testing machine of pure HDPE, 5% BPP (Banana peel powder) filled, 10% BPP filled and 15% BPP filled composites are shown in figure 1, figure 2, figure 3, and figure 4 respectively. Figure 1 indicates the sample with pure HDPE for tensile strength. The brake load and peak load was obtained at 246N length 11.2MM and 550 N at length 9.1 MM respectively. The figure 2 indicates the sample with 5% banana peel powder and the remaining percentage is HDPE for tensile strength. The brake load and peak load was obtained at 128 N length 10.2 MM and 550 N at length 9.0 MM respectively. The figure 3 indicates the sample with 10% banana peel powder and the remaining percentage is HDPE for tensile strength. The brake load and peak load was obtained at 108 N length 5.4 MM and 432 N at length 4.2 MM respectively. The figure 4 indicates the sample with 15% banana peel powder and the remaining percentage is HDPE for tensile strength. The brake load and peak load was obtained at 108 N length 7.9 MM and 510 N at length 7.5 MM respectively.

The tensile strength results in table 3 for composite sample which are prepared with BPP filler in different volumes fraction the load versus displacement curve illustrate that the maximum tensile strength is obtained for the composite prepared with 5% volume fraction. Banana peel powder HDPE composite with the higher fraction of filler 15% has the lowest strength this may be due to imperfect interfacial bonding between BPP and HDPE to transfer tensile strength.

The experimental curves for bending strength from tensometer testing machine of 5% BPP filled, 10% BPP filled and 15 % BPP filled composites are shown in figure 5, figure 6, figure 7, and figure 8 respectively. Figure 5 specifies the sample with pure HDPE for bending strength. The brake load and peak load was obtained at 216N length 10.6MM and 608N at length 9.3 MM respectively. Figure 6 gives the sample with 5% banana peel powder and the remaining percentage is HDPE for bending strength. The brake load and peak load was obtained at 0 N length 0.0 MM and 39 N at length 6.2 MM respectively. The figure 7 illustrates the sample with 10% banana peel powder and the remaining percentage is HDPE for bending strength. The brake load and peak load was obtained at 0 N length 0.0 MM and 30 N at length 3.9 MM respectively. The figure 8 shows the sample with 10% banana peel powder and the remaining percentage is HDPE for bending strength. The brake load and peak load was obtained at 39 N length 0.1 MM and 39 N at length 0.1 MM respectively.

The bending strength results in table 3 for composite sample which are prepared with BPP filler in different volumes fraction the load versus displacement curve illustrate that the maximum bending strength is obtained for the composite prepared with 15% volume fraction. Banana peel powder HDPE composite with the higher fraction of filler 5% has the lowest strength this may be due to imperfect interfacial bonding between BPP and HDPE to transfer tensile strength.

The impact strength of 5% BPP filled, 10% BPP filled and 15 % BPP filled composites of its strengths are shown in the following table 6. The impact strength results in table 6 for composite sample which are prepared with BPP filler in different volumes fraction the load versus displacement curve illustrate that the maximum impact strength is obtained for the composite prepared with 10% BPP volume fraction. The banana peel powder HDPE, composite with the higher fraction of filler 15% has the lowest strength this may be due to imperfect interfacial bonding between BPP and HDPE to transfer tensile strength. Therefore, it is common for impact strength to be higher than the tensile strength for the same composite sample. Table 6 gives the Impact strength of the composite sample. The maximum impact strength obtained was at 10% composite

- CONCLUSION

The experimental characterization of banana peel powder for composite leads to the maximum tensile strength is obtained for the composite prepared with 5% BPP volume fraction and lower strength is obtained for the composite prepared with 10% volume fraction of BPP, the maximum bending strength is obtained for the composite prepared with 15% BPP volume fraction and lower strength is obtained for the composite prepared with 10% volume fraction of BPP,  the maximum impact strength is obtained for the composite prepared with 10% BPP volume fraction and lower strength is obtained for the composite prepared with 15% volume fraction. The composite is prepared with 5% BPP is good for tensile applications, 10% BPP is good for impact applications and 15% BPP is good for bending applications. Banana peel powder for hybrid composite can be used as an alternative material for the interiors of aircraft, spacecraft, ships, electronics, and automobiles.

- ACKNOWLEDGMENT

We have gratefully acknowledged the staff of V. R. Siddhartha College of Engineering, Vijayawada, Andhra Pradesh India for providing us with test facility. Authors also express their thankfulness to Mr. Manoj Kumar, former Junior Research Fellow & Ph.D. Scholar, Department of Biotechnology, VFSTR University, India and at present with Fachbereich Molekulare Biotechnologie (FH Campus Wien; https://www.fh-campuswien.ac.at), Wien, Austria for his help while preparing the samples.

- REFERENCES

[1] Karal Ziegler Nature Materials 12, 773 (2013)

[2] Duan X, Cheng G, Yang E, et al. Food Chemistry. 2008; 111(1): 144-149.

[3] A. Alavudeen, N. Rajini, S. Karthikeyan, M. Thiruchitrambalam, N. enkateshwaren. M & D, 66(A), 246-257, (2015).

[4] V. Arumuga Prabhu, M. Uthayakumar, V. Manikandan, N. Rajini, P. M & Design, Volume 64, December 2014, Pages 270-279.

[5] M. Boopalan, M. Niranjana, M.J. Umapathy composites Part B: Engineering, Volume 51, August 2013, Pages 54-57.

## [6] M. Ramesh, T. Sri Ananda Atreya, U.S. Aswin, H. Eashwar, C. Deepa rocedia Engineering, Volume 97, 2014, Pages 563-572.

[7] P. Tixier, F. Salmon, C. Chabrier, P. Protection, Volume 27, Issue 11, November 2008, Pages 1427-1431.

## [8] A.A. Mamun, H.P. Heim, O. Faruk, A.K. Bledzki Biofiber Reinforcements in composite Materials, 2015, Pages 236-272.

[9] T. H. Emaga, R. H. Andrianaivo, B. Wathelet, J. T. Tchango and M. Paquot, Food chemistry, vol. 103, no. 2, (2007), pp. 590-600.

[10] V.P. Arthanarieswaran, A. Kumaravel, M. Kathirselvam Materials & Design, Volume 64, December 2014, Pages 194-202.

[11] Vishnu Prasad, Ajil Joy, G. Venkatachalam, S. Narayanan, S. Rajakumar Procedia Engineering, Volume 97, 2014, Pages 1116-1125.

[12] N. Venkateshwaran, A. Elaya Perumal, A. Alavudeen, M. Thiruchitrambalam Materials & Design, Volume 32, Issue 7, August 2011, Pages 4017-4021.

[13] R. Bhoopathi, M. Ramesh, C. Deepa Procedia Engineering, Volume 97, 2014, Pages 2032-2041.

[14] J. J. H. Nusselder and H. M. C. Stijnen, European Patent No. EP 1681147. Munich, Germany: European Patent Office, (2006).

[15] Maries Idicula, S.K. Malhotra, Kuru villa Joseph, Sabu Thomas Dynamic composite Science and Technology, Volume 65, Issues 7–8, June 2005, Pages 1077-1087

[16] Pranav D. Pathak, Sachin A. Mandavgane, Journal of Environmental Chemical Engineering, Volume 3, Issue 4, Part A, December 2015, Pages 2435-2447.

[17] Jean-Marc Blazy, Philippe Tixier, Alban Thomas, Harry Ozier-Lafontaine, Frédéric Salmon, Agricultural Systems, Volume 103, Issue 4, May 2010, Pages 221-232.

[18] Glyn Harper, Ganesh Dahal, George Thottappilly, R. Hull Journal of Virological Methods, Volume 79, Issue 1, 1 April 1999, Pages 1-8.

## [19] Yunia Verónica García-Tejeda, et al Food Science, and Technology, Volume 54, Issue 2, December 2013, Pages 447-455.

## [20] P. Tixier, F. Salmon, C. Chabrier, P. Crop Protection, Volume 27, Issue 11, November 2008, Pages 1427-1431.

[21] N. Cordeiro, C. Mendonça, L.A. Pathan, A. Carbohydrate Polymers, Volume 88, Issue 1, 17 March 2012, Pages 125-131.

- FIGURES:

Fig. 1. Load versus displacement curve of pure HDPE for tensile strength

Fig. 2. Load versus displacement curve of 5% BPP composite for tensile strength

Fig. 3. Load versus displacement curve of 10% BPP composite for tensile strength

Figure 4. Load versus displacement curve of 15% BPP composite for tensile strength

Fig. 5. Load versus displacement curve of pure HDPE for bending strength

Fig 6. Load versus displacement curve of 5% BPP composite for bending strength

Fig. 7. Load versus displacement curve of 10% BPP composite for bending strength

Fig. 8. Load versus displacement curve of 15% BPP composite for bending strength

- TABLES

Table 1 Shapes and dimensions of composite sample

| Composite sample | Shape | Dimensions |
| --- | --- | --- |
|  | . | Length = 12.4 cm Thickness= 3 mm Edges width =1.85 cm Middle width =1.3 cm |
|  |  | Length= 9.5 cm Thickness= 3 mm Width = 1 cm |
|  |  | Length = 6.2 cm Width = 1 cm Thickness= 9 mm |

Table 2. Load and displacement of tensile test Composites

| Composite sample | Peak load in N | Break load in N | Peak load Displacement in MM | Break load Displacement in MM |
| --- | --- | --- | --- | --- |
| Pure HDPE | 550 | 246 | 9.1 | 11.1 |
| 5% BPP filled | 550 | 128 | 9.0 | 10.2 |
| 10% BPP filled | 432 | 108 | 4.2 | 5.4 |
| 15% BPP filled | 510 | 108 | 7.5 | 7.9 |

Table 3. Tensile strength of composite sample

| Composite sample | Tensile strength in N/SQ MM |
| --- | --- |
| Pure HDPE | 13.1 |
| 5% BPP filled | 13.8 |
| 10% BPP filled | 10.8 |
| 15% BPP filled | 12.8 |

# Footnotes

Aradhyula Thirumala Vasu1is with 1 Department of Mechanical Engineering, Vignan’s Foundation for Science, Technology and Research University (VFSTRU; Vignan University), Vadlamudi, Andhra Pradesh 522 213 India (corresponding author’s phone:+91-8179678131; e-mail:aradhyulat@gmail.com).

Ram Narayan Chauhan 2, 2 Photonics Division, National Chiao Tung University, 1001 University Road, Hsinchu, Taiwan 300 ROC(chauhanramnarayan@gmail.com)

M. Ramakrishna1 is with 1 Department of Mechanical Engineering, Vignan’s Foundation for Science, Technology and Research University (VFSTRU; Vignan University), Vadlamudi, Andhra Pradesh 522 213 India (corresponding author’s e-mail:drmramakrishna@gmail.com).

Murthy Chavali3*. 3* Division of Chemistry, Department of Sciences and Humanities, Vignan’s Foundation for Science, Technology and Research University (VFSTRU; Vignan University), Vadlamudi, Andhra Pradesh 522 213 India